Estimate Factors

Item No. 			Description 						Factor

AGGREGATE BASE COURSE

304-01.____ 	Type 1 Aggregate for Base (__ in. Thick)				0.058 Tons/yd2/inch Compacted

304-05.04 	Type 5 Aggregate for Base (4 in. Thick)				0.22 Tons/yd2 Compacted

Total Weight of Base Material at Optimum Moisture Content

AGGREGATE SURFACE

310-____ 	Gravel, Crushed Stone and Chat					0.039 Ton/yd2/inch or

0.028 yd3/yd2/inch (Based on

1.40 Tons/yd3 of loose Aggregate)

PLANT MIX BITUMINOUS BASE COURSE

401-30.00 	Bituminous Pavement Mixture PG64-22 (Base)			1.943 Ton/yd3 Compacted Mixture

401-30.10 	Bituminous Pavement Mixture PG64-22 (Base Widening)		1.943 Ton/yd3 Compacted Mixture

PLANT MIX BITUMINOUS PAVEMENT

401-12.09A 	Bituminous Pavement Mixture PG64-22 (BP-1)			1.948 Ton/yd3 Compacted Mixture

401-12.11A 	Bituminous Pavement Mixture PG64-22 (BP-2)			1.934 Ton/yd3 Compacted Mixture

401-12.11A 	Bituminous Pavement Mixture PG64-22 (BP-3)			1.893 Ton/yd3 Compacted Mixture

PLANT MIX BITUMINOUS SURFACE LEVELING

402-05.20A 	Bituminous Pavement Mixture PG64-22

(Obtain Factors from District Operations)

ASPHALTIC CONCRETE PAVEMENT

403-____ 	Asphaltic Concrete Mixture (Type SP095 Mix)			1.913 Ton/yd3 Compacted Mixture

403-____ 	Asphaltic Concrete Mixture (Type SP125 Mix)			1.927 Ton/yd3 Compacted Mixture

403-____ 	Asphaltic Concrete Mixture (Type SP190 Mix)			1.940 Ton/yd3 Compacted Mixture

403-____ 	Asphaltic Concrete Mixture (Type SP250 Mix)			1.946 Ton/yd3 Compacted Mixture

403-____ 	Asphaltic Concrete Mixture (Type SP095 SMA Mix)			1.930 Ton/yd3 Compacted Mixture

403-____ 	Asphaltic Concrete Mixture (Type SP125 SMA Mix)			1.965 Ton/yd3 Compacted Mixture

PROCESSING RECLAIMED ASPHALT

405-10.01 	Liquid Asphalt MC 250						12.8 Gal/Ton of Aggregate

TACK COAT

407-10.05 	New Asphalt Surfaces						0.05 Gal/yd2

407-10.05 	Existing Asphalt or Concrete Surfaces				0.08 Gal/yd2

407-10.05 	Coldmilled Asphalt or Concrete Surfaces				0.10 Gal/yd2

PRIME COAT

408-10.____ 	Prime								0.35 Gal/yd2 (Aggregate Base)

0.25 Gal/yd2 (Color Coat)

SEAL COAT

409-10.___ 	Seal Coat, Grade ___ 						0.25 – 0.40 Gal/yd2

NA		Cover Aggregate

Light Weight Aggregate					12 lb/yd2

Limestone							17 lb/yd2

Porphyry							22 lb/yd2

NOTE:  These factors are statewide average estimates and should be used only for preliminary estimates.  Mix designs have

been established for most rock formations and the designer should request specific factor recommendations from the

district operations engineer.

Revised 02/27/18